# Metallic Additive Product Training

| SOP ID | PEC-OPS-002 |
| --- | --- |
| Company | Prescott Epoxy Company (PEC) |
| Department | OPS |
| Version | 1.0 |
| Effective Date | 2026-04-13 |
| Owner | Dylan Nordby |

## Purpose

Provide installers with product knowledge, mixing procedures, and application techniques for Simiron Metallic Additive to ensure consistent, high-quality metallic floor installations.

## Scope

All PEC installers working with metallic epoxy systems.

## Tools and Materials

- Simiron Metallic Additive pigment (32 oz per 3-gallon kit)

- Simiron 1100 SL clear epoxy with slow cure activator

- Drill with Jiffy-style mixing blade

- Weenie roller and frame

- 18-inch roller and frame

- Measuring cups

- PPE (gloves, respirator, glasses, long sleeves)

- Cleats

## Procedure

### Product Overview

Simiron Metallic Additive is a pigment system that can be added to Simiron clear epoxies that cure at a moderate/slow rate.

When dispersed within the coating, the exotic pigment creates a beautiful three-dimensional appearance that gives the illusion of waves, swirls, and ripples.

The finished appearance of the metallic flooring system can vary from gradual, subtle changes in color to more distinctive effects. Each project is truly unique.

### Approved Uses

- Restaurants and bars

- Sports arenas

- Showroom floors

- Residential homes

- Lobbies

- Hair studios

- Garages

- Restrooms

- Schools and universities

### Temperature Limitations

Surface, product, and air temperatures must all be within range before, during, and after application.

- Air temperature: 60-85 degrees Fahrenheit

- Surface temperature: 60-85 degrees Fahrenheit

- Material temperature: 60-85 degrees Fahrenheit

### Mixing Instructions

- 24 hours before the project, mix 32 oz of metallic epoxy coloring into a 3-gallon kit to avoid fish eyes and shooting stars in the metallic product.

- The next day at the project (after prep), mix with a slow cure activator to the same specs as a regular 1100 SL project.

- Make sure all additives are mixed in before pouring out the product.

- DO NOT allow the product to sit in the bucket as this can cause it to fire off in the bucket.

### Application Instructions

- This coating goes over a base coat that compliments the top metallic coat in case of thinner or thicker spots that need covered.

- Measure out 150 square feet for each 3-gallon kit on the project.

- Only pour and spread your metallic in that measured area. If you are unsure you will make it to the next square/stopping point, have another kit being mixed as your metallic is being poured and laid down.

- After pouring the product, have one person use a weenie roller and swirl into edges.

- Have one person in the field swirling the epoxy. Having too many people on the floor will make it look less uniform and the pattern will change as you go.

- Keep your swirls and lines going the same way for consistency.

### Common Mistakes

- Not pre-mixing the metallic pigment 24 hours ahead, causing fish eyes and shooting stars

- Allowing mixed product to sit in the bucket, causing it to fire off

- Having too many people on the floor, creating inconsistent patterns

- Not maintaining consistent swirl direction throughout the application

- Running out of mixed material mid-section without a backup kit ready

## Revision History

| Date | Author | Changes |
| --- | --- | --- |
| 2026-04-13 | Dylan Nordby / SOP Manager | Initial version created from training documentation. |

Source: SOP Hub | Generated 2026-04-13