# High Wear Urethane Product Training

| SOP ID | PEC-OPS-003 |
| --- | --- |
| Company | Prescott Epoxy Company (PEC) |
| Department | OPS |
| Version | 1.0 |
| Effective Date | 2026-04-13 |
| Owner | Dylan Nordby |

## Purpose

Train installers on proper mixing, application, and surface prep for Simiron SimThane HWU to prevent coating defects and ensure long-term durability.

## Scope

All PEC installers applying HWU topcoats.

## Tools and Materials

- Simiron SimThane HWU (Part A, Part B, Part C filler)

- Simiron tint pack (optional, 1 per gallon kit)

- Drill with Jiffy-style mixing blade

- Roller pan

- 3/8-inch nap roller

- Small edging roller

- Brush for cutting in

- 80-120 grit sanding screens

- Vacuum

- Acetone and rags

- Spiked shoes

- PPE (gloves, safety glasses, respiratory protection)

## Procedure

### Product Overview

Simiron SimThane HWU is a high-performance, three-component, high-solids, low-VOC urethane floor coating designed for extreme durability. It provides superior resistance to abrasion, chemicals, corrosion, and UV exposure while maintaining flexibility.

This product is supplied as a neutral satin topcoat with a light, consistent texture. It can be tinted using one Simiron tint pack per one-gallon kit.

This coating does not self-level or hide defects. Whatever is visible during application will cure into the floor.

### Approved Uses

SimThane HWU is designed as a topcoat only and must be applied over properly prepared epoxy systems.

- Topcoat for epoxy systems

- Industrial and commercial warehouses

- Manufacturing facilities

- Automotive service areas

- High-traffic floors

- Hangars

- Shop floors

- Garages

### Environmental and Temperature Requirements

Surface, product, and air temperatures must all be within range before, during, and after application.

- Surface temperature: 60-85 degrees F

- Product temperature: 60-85 degrees F

- Air temperature: 60-85 degrees F

- Do not apply outside of these ranges.

### Mixing Instructions (Critical)

SimThane HWU is a three-component system. Follow the order exactly.

- Pre-mix Part B at low speed using a drill and Jiffy-style mixing blade.

- If pigmenting, add one Simiron tint pack per gallon kit to Part B and mix until fully dispersed.

- Slowly add Part C filler and mix for 3 minutes until evenly blended.

- Add Part A and mix for an additional 3 minutes.

- Do not mix more than one kit at a time.

Improper mixing will cause color, texture, and performance issues.

### Application Instructions

General Application Notes

- Target coverage rate: 600 sq ft per gallon.

- Apply thin. Thicker application increases the risk of bubbles, soft film, gloss variation, and texture issues.

- This product does not flow out. Defects must be corrected while wet.

Step-by-Step Application

- Cut in edges, coves, and obstructions using a brush. Apply very thin at coves and vertical transitions. Material will run on vertical surfaces and pool at the base. Roll these areas out with a small edging roller if needed.

- Pour mixed material into a roller pan.

- Apply using a 3/8-inch nap roller. Dip roller and lightly roll off excess material. Roll 2 parallel paths (left to right or right to left), approximately 8-10 feet long. Repeat until there are 4 adjacent roller paths in front of the applicator.

- Frequently agitate material in the roller pan. Part C filler settles quickly. Rolling excess filler from the bottom of the pan can cause color and texture inconsistencies.

- Back-roll perpendicular to the original passes using a V-pattern. This evens out material and removes roller lines. Final passes should be straight up and back. Pull material toward yourself and overlap at least 1 foot into the previous section.

- Continue working across the floor. Minimize time between tie-ins. Use control joints or natural breaks between mixes.

- Optional finish rolling: A second installer may finish roll no more than 20 minutes behind the main applicator. Must be on spiked shoes. Pull a wet roller across the entire area in the same direction as original passes.

- Inspect constantly. Reroll any areas that do not look acceptable before the product tacks.

### Surface Preparation Requirements

SimThane HWU must be applied over a properly prepared epoxy or moisture vapor barrier system.

- Ensure epoxy or MVB coating has fired off before topcoating.

- Sand existing coating with 80-120 grit sanding screens.

- Vacuum thoroughly.

- Inspect the surface carefully. This product does not hide defects. All imperfections will show.

- Perform a detailed vacuum followed by an acetone wipe.

- Allow acetone to fully flash off before coating.

- Once surface is clean, dry, and defect-free, proceed with application.

### What You Cannot Do

- Do not apply over smooth epoxy.

- Do not apply over bare concrete. This will result in peeling and failure.

- Do not reroll material that has begun to tack.

- Do not mix more than one kit at a time.

- Do not allow filler to settle in the roller pan.

- Do not coat over oil, dust, or any debris.

- Do not apply thicker than the recommended coverage rate.

### Common Mistakes to Avoid

- Rolling back into tacky material, causing lines or orange peel.

- Applying too much product, which can lead to peeling.

- Letting filler settle in the pan, causing uneven texture and color.

- Placing items on the floor before full cure.

- Assuming defects will flow out. They will not.

### Key Takeaways for Installers

- Prep determines final appearance.

- Thin application is mandatory.

- Work clean and methodically.

- Watch your timing. Once it tacks, leave it alone.

- What you see wet is what you get cured.

## Revision History

| Date | Author | Changes |
| --- | --- | --- |
| 2026-04-13 | Dylan Nordby / SOP Manager | Initial version created from training documentation. |

Source: SOP Hub | Generated 2026-04-13