# Polyaspartic HS Product Training

| SOP ID | PEC-OPS-004 |
| --- | --- |
| Company | Prescott Epoxy Company (PEC) |
| Department | OPS |
| Version | 1.0 |
| Effective Date | 2026-04-13 |
| Owner | Dylan Nordby |

## Purpose

Standardize mixing, application, and surface prep for Simiron Polyaspartic HS to ensure consistent film build and avoid common defects like hazing, fire-off, and uneven coverage.

## Scope

All PEC installers applying polyaspartic topcoats over broadcast systems.

## Tools and Materials

- Simiron Polyaspartic HS (Base and Activator in chosen cure speed)

- Drill with Jiffy-style mixing blade

- Flat squeegee

- 3/8-inch nap 18-inch roller and frame

- Dip tray (for high humidity)

- Chip brush for edges and joints

- Simiron Aluminum Oxide (for solid color systems)

- Cleats

- PPE (gloves, safety glasses, respiratory protection)

## Procedure

### Product Overview

Simiron Polyaspartic HS is a two-component, high-performance, aliphatic polyaspartic floor coating designed for application up to 16 mils in a single pass over full broadcast systems.

This product provides superior adhesion, durability, and resistance to stains, chemicals, abrasion, and UV exposure, making it suitable for both interior and exterior environments.

Polyaspartic HS is available in multiple cure speeds to allow installers to adapt to temperature, humidity, crew size, and job complexity.

### Cure Speed Options

- XTRA Slow Cure: Extended working time. Designed for extremely hot and/or humid environments.

- Slow Cure: Longer working time. Ideal for less experienced applicators or installations requiring additional work time.

- Medium Cure: Balanced work and cure time. Suitable for most standard conditions.

- Fast Cure: Reduced work and cure times. Intended for experienced installers, large crews, or projects requiring rapid return to service.

### Approved Uses

Designed as a protective topcoat over properly prepared broadcast systems and epoxy bases.

- Full flake broadcast systems

- Full quartz broadcast systems

- Solid color epoxy systems when combined with Simiron Aluminum Oxide for added slip resistance

- Interior and exterior floor coatings exposed to UV

### Temperature Limitations

All temperatures must be within range at time of application.

- Surface temperature: 35-85 degrees F

- Product temperature: 60-85 degrees F

- Air temperature: 35-85 degrees F

- Select cure speed appropriately for conditions.

### Mixing Instructions

- Mix 1:1 by volume (Base to Activator).

- Use a low-speed drill with a Jiffy-style mixing blade.

- Mix for 3 minutes or until uniform.

- Avoid introducing air during mixing. Excess air can cause premature reaction and shortened working time.

- Do not mix more material than can be applied within the working time.

Improper mixing may result in product firing off too quickly, incomplete cure, or surface defects/haze.

### Application Instructions

Coverage Rates

- Apply at 100-160 square feet per gallon.

- Maintain consistent film thickness.

- Do not exceed recommended spread rates.

Application Method

- Spread material using a flat squeegee to evenly distribute product.

- Back-roll: Begin at the furthest point from the mixing area. Use a 3/8-inch nap, 18-inch roller. Maintain a half-roller overlap.

- Cross-roll: Roll perpendicular to initial direction. Use the same roller and overlap.

- High humidity conditions: Use a dip tray and dip-and-roll method. Apply at same coverage rates as squeegee application.

- Joint and edge control: Use joints as natural breaks between sections. Brush out joints to prevent overfilling. Pay close attention to edges and transitions to maintain even coverage.

Overfilled joints can lead to clouded or foggy areas in the finished coating.

### Surface Preparation Requirements

- Over solid epoxy coatings: Sand or grind to 80-100 grit profile.

- Over full flake or quartz broadcast: Scrape loose aggregate, then thoroughly vacuum surface.

- Recoating existing polyaspartic: Sand at 60 grit to achieve proper mechanical profile before applying additional coats.

- Surface must be clean, dry, and free of contaminants prior to application.

### What You Cannot Do

- Do not apply as a topcoat for smooth floor systems. Designed for full broadcast systems only (flake, quartz, silica sand).

- Do not apply outside recommended temperature ranges. Use Fast Cure for cooler conditions.

- Do not apply over loose or unsound concrete, asphalt or bitumen substrates, glazed tile or nonporous brick, magnesite, copper or metal substrates, or polyester or elastomeric membranes.

- Do not ignore moving joints or shrinkage cracks. These may reflect through the finished system if not honored.

- Do not apply thicker than recommended or allow material to pool. This can cause a white or hazy appearance.

- Do not allow product to freeze.

### Common Mistakes to Avoid

- Overmixing or undermixing material.

- Walking back into coating after cross-rolling.

- Recoating over unsanded polyaspartic.

- Leaving residual flake, quartz, dust, or contaminants on the surface.

- Introducing excess air through high-speed mixing.

- Pouring full buckets in high humidity conditions, causing rapid fire-off.

## Revision History

| Date | Author | Changes |
| --- | --- | --- |
| 2026-04-13 | Dylan Nordby / SOP Manager | Initial version created from training documentation. |

Source: SOP Hub | Generated 2026-04-13