# Simiron 1100 SL Product Training

| SOP ID | PEC-OPS-005 |
| --- | --- |
| Company | Prescott Epoxy Company (PEC) |
| Department | OPS |
| Version | 1.0 |
| Effective Date | 2026-04-13 |
| Owner | Dylan Nordby |

## Purpose

Train installers on proper mixing ratios, coverage rates, pigmenting, and application techniques for Simiron 1100 SL across all system types.

## Scope

All PEC installers working with 1100 SL basecoat epoxy.

## Tools and Materials

- Simiron 1100 SL (Part A base, Part B activator)

- E-Tint pigment packs

- Drill with Jiffy-style mixing blade

- 1/8-inch notched squeegee

- Flat squeegee

- 3/8-inch nap 18-inch roller and frame

- 6-inch weenie roller and frame

- Chip brush for edges

- Measuring cups

- Cleats

- PPE (gloves, safety glasses, respiratory protection)

## Procedure

### Product Overview

Simiron 1100 SL is a 100% solids, self-leveling epoxy used as a basecoat and system component across multiple PEC floor systems.

### Activator Options

- Fast Cure: Used in colder temperatures, when faster cure times are required, and when using thickening fibers for crack repair or spalling.

- Medium (Regular) Cure: Standard activator. Used for flake systems, quartz systems, solid color systems, and grind and seal systems.

- Slow Cure: Used specifically for metallic systems. Allows extended working time and better movement of metallic pigments.

### Approved Uses

- Basecoat for epoxy flake systems

- Basecoat for epoxy quartz systems

- Basecoat for solid color epoxy systems

- Basecoat for metallic epoxy systems

- Basecoat for grind and seal systems

- Crack and spall repair when combined with thickening fibers and fast cure activator

### Temperature Limitations

All three temperatures must be within range before installation.

- Air temperature: 35-85 degrees F

- Surface temperature: 35-85 degrees F

- Material temperature: 60-85 degrees F

- Do not install if any of these fall outside the approved range.

### Mixing Instructions

- Pre-mix Part A (Base) at low speed for 1 minute. If pigmenting, add E-Tint pigment during this step.

- Add Part B (Activator). Mix for 3 minutes until fully uniform. Scrape sides and bottom during mixing.

- Batch Size Rule: Do not mix more material than can be applied in 10-15 minutes. Material will stiffen and tack up if left in the bucket too long.

### Coverage Rates (Critical)

Measure the space before mixing to calculate exact material needs.

- Metallic systems: 53 square feet per gallon

- Flake, quartz, solid color, grind and seal: 160 square feet per gallon

### Mix Ratios

- 2 parts Base : 1 part Activator

- Measure accurately every time

### Pigmenting Guidelines

- Pre-pigmented product: Mix base + activator for 3 minutes.

- Unpigmented product: Add 1 pigment pack per gallon of base. Mix base + pigment for 1 minute. Add activator. Mix for 3 minutes.

### Placement and Spreading

- Immediately pour material out of the bucket onto the floor. Pour into individual sections based on calculated square footage.

- Do not dump excess material into joints. Use material already in the joint to coat it. Pull excess out of joints immediately.

- Spread with squeegee. Use 1/8-inch notched squeegee. Hold at an angle. Work toward your exit path.

- Cut in edges and joints. Use a chip brush for edges and joint control.

- Back roll. Use a 3/8-inch nap, 18-inch roller. Half-roller overlap. Start at first pour area and work outward.

- Cross roll. Same roller and overlap. Ensure uniform coverage. Recheck joints and edges for consistency.

### Surface Preparation Requirements

- Grind entire surface to a 16/18 grit profile.

- Concrete must show open pores with no cream or laitance remaining.

- Patch all surface imperfections dime-size or larger.

- Follow PEC patching procedures (see PEC-OPS-007).

### What You Cannot Do

- Do not back roll epoxy that has become sticky or tacky. This will affect self-leveling and color consistency.

- Do not apply over rust, dust, unstable concrete, or extreme spalling/hollow spots.

- Do not allow control joints to overfill. Excess material can cause cracking or joint pull-through.

- Do not allow product to freeze at any time.

### Common Mistakes to Avoid

- Overfilling control joints.

- Applying too much material to the floor. Always follow spread rate guidelines. Excess material must be removed before continuing.

- Undermixing material. Pigmented clear base needs 1 minute with pigment + 3 minutes after activator. Pre-pigmented base needs full 3 minutes with activator.

- Leaving mixed epoxy sitting in a bucket. Buckets shorten pot life. Product will fire off faster if left sitting on the ground.

## Revision History

| Date | Author | Changes |
| --- | --- | --- |
| 2026-04-13 | Dylan Nordby / SOP Manager | Initial version created from training documentation. |

Source: SOP Hub | Generated 2026-04-13