# Concrete Patching Procedures

| SOP ID | PEC-OPS-007 |
| --- | --- |
| Company | Prescott Epoxy Company (PEC) |
| Department | OPS |
| Version | 1.0 |
| Effective Date | 2026-04-13 |
| Owner | Dylan Nordby |

## Purpose

Define patching scope, materials, and techniques to ensure proper repair of concrete defects before coating application.

## Scope

All PEC installers performing concrete repair and patching.

## Tools and Materials

- Simiron 1100 SL base (clear)

- Simiron 1100 SL fast cure activator

- Thickening fibers

- Instant Patch (A and B components)

- Sand (for instant patch fill)

- UniPro/Henrys Quick Patch

- Feather Finish

- Measuring cups

- Paint sticks

- Razor scraper

- Hand grinder

- PPE (gloves, masks, long sleeves, safety glasses/goggles)

## Procedure

### What Do We Patch?

- New concrete with on-site estimate: We will patch all cracks. If there are extensive cracks, it will be figured into the estimate.

- Under existing coatings or off-site estimates: Does not include cracks wider than 1/8 inch, or spalls deeper than 1/4 inch or larger than 3 inches in diameter.

### Epoxy Paste Patch

USE PROPER PPE WHEN USING ANY CHEMICAL PATCH: gloves, masks, long sleeves, and safety glasses/goggles.

- Measure out a 2:1 ratio of clear Simiron 1100 base (2) to Simiron 1100 SL fast cure activator (1) in separate cups. Make sure measurements are accurate.

- In the base cup, mix in thickening fibers to a consistency of peanut butter. Mix until thoroughly incorporated.

- Add the full amount of activator using paint sticks to pull the full amount into the other cup.

- Mix for 3 minutes to thoroughly incorporate all products.

- After mixing, immediately walk to all noted patch points and fill larger cracks/spalls in the field.

- The initial patch will sink, so use more than you think you need.

- Go back through to scrape/grind excess product off the top for a smooth and continuous floor profile.

This is VERY important for quartz, solid color epoxy coatings, and grind and seals for the cleanest final product. Flake will cover smaller imperfections but do your due diligence.

This epoxy paste can be coated over wet or cured, but if cured it will need a grind for a scratch profile unless still in the 24-hour coating period.

This product can be used over other epoxy coatings if needed for on-site fixes before topcoat.

If coating over this product, allow it to cure before coating over.

### Instant Patch

USE PROPER PPE. ONLY USE ON CONCRETE WITH NO COATING. This product needs a concrete substrate to latch and properly adhere to prior to over-coating.

- Measure at a 1:1 ratio between A and B.

- If filling anything that needs more structure, you can use sand to make a somewhat stronger material.

- If using sand, you will most likely need to grind after patching for a smoother finish.

- Use mostly in smaller hairline cracks or spalls that have no extended deeper delamination/failure.

- Can also be used to fill joints if needed for polishing or metallic coatings. Make sure there is an aggressive enough scratch on anything you plan on patching.

- If filling control joints, fill with sand about halfway to the top, then fill the rest with this patch. Grind/scrape to a flat profile before over-coating/polishing.

- If mixed improperly, there will be an oily film on the surface.

### UniPro / Henrys Quick Patch

- A concrete-like patch that should only be used for light traffic patches like in corners or along sides of garages where foot traffic will not affect the structure.

- Use on patches no bigger than a dime or hairline cracks no larger than 3 inches long and 1/8 inch wide.

### Feather Finish

Used mostly for polishing when you need to pull something as tight as possible for a smooth floor project.

Can be polished after allowing it to fully cure, or coated over as long as it is fully cured.

Only use as recommended on bags. This is a specialty project order.

## Revision History

| Date | Author | Changes |
| --- | --- | --- |
| 2026-04-13 | Dylan Nordby / SOP Manager | Initial version created from training documentation. |

Source: SOP Hub | Generated 2026-04-13