# Concrete Grinding Procedures

| SOP ID | PEC-OPS-008 |
| --- | --- |
| Company | Prescott Epoxy Company (PEC) |
| Department | OPS |
| Version | 1.0 |
| Effective Date | 2026-04-13 |
| Owner | Dylan Nordby |

## Purpose

Train installers on concrete hardness assessment, diamond selection, grinding techniques, and troubleshooting to ensure proper surface preparation for all coating systems.

## Scope

All PEC installers operating grinding equipment.

## Tools and Materials

- Propane grinder (industrial)

- 7-inch hand grinder with shroud

- 4-inch grinder with shroud

- Vacuums (for hand units and industrial unit)

- Diamond segments (various bonds and grits)

- PCD wheels/diamonds

- 4-inch V-blade wheel

- Mohs hardness test kit

- Respirators

- PPE (masks, gloves, knee pads, glasses)

## Procedure

### Concrete Hardness

- The hardness of concrete is measured on the Mohs hardness scale (1 = softest, 10 = hardest).

- The most common concrete hardness in our area is Mohs 7, but can go slightly higher or way softer.

- This is the first thing to assess. It determines everything about diamond tooling selection.

- Key rule: Soft concrete takes hard diamonds. Hard concrete takes soft diamonds.

### Diamond Bond Types

- SS/Super Soft: Used for concrete with Mohs 7-8. Recommend super soft single seg 16/18 diamonds for maximum cutting force on harder floors.

- S/Soft: Used for Mohs 5-6. Use 16/18 for epoxy coatings. Use 30/40 soft double seg or double dot for first step of a polish system.

- M/Medium: Used mostly on Mohs 4-5. If not pulling enough cream, switch to soft bond for harder concrete or hard bond for softer concrete.

- H/Hard: Used for anything less than Mohs 4. These do not dig too deep in softer concrete. Mostly used on self-leveling concrete (rarely used in the field).

### Segment Patterns

- Single seg/single dot/single arrows: Pull more cream off. Less diamond contact means less smoothing and a more aggressive scratch.

- Double seg/double dot/double arrows: Less aggressive scratch/smoother floors. More contact causes more smoothing.

- PCD wheels/diamonds: Pull up coatings or overlays much more efficiently. Use a tooth to pull up coatings and a bar to smooth the concrete. After PCD use, may need to smooth with double/single seg 16/18 or 30/40.

### Diamond Grit Sizes

- 16/18: Most aggressive. Best grip for coatings as it leaves deeper scratches for epoxy to bond.

- 30/40: Step above 16/18. Used for grind and seals.

- 60/80: Used for grind and seals based on product representative recommendations.

- Anything higher is getting into polishing systems.

### Diamond Color Guide

- Black diamonds: Super soft bond

- Purple diamonds: Soft bond

- Green diamonds: Medium bond

- Grey diamonds: Typically used for PCDs

- 7-inch grinder wheels are selected based on diamond type rather than hardness, except specialty wheels like purple PCD or orange creamsicle 16/18 for hard concrete.

### General Grinding Procedures

- Check concrete hardness first. This tells you everything about tooling needed.

- Select the right bond diamond and tooling type based on your end product goal.

- Check vacuum suction before turning on the grinder. Wear respirators if there is not adequate suction.

- Once suction is checked, vacuums are purged, and respirators are on, start grinding.

- In the field with the big grinder: Go slow enough to take off enough cream to see aggregate (for coatings) or desired cut pattern (for polishes). Overlap halfway with every cut. Purge vacuum as you go.

- For edges: Hit corners first. Keep your grinder flat and work out gouges/dips by making circles. Do not allow the grinder to sit in one spot. Hand grinders gouge way easier than orbital propane grinders.

- When finished with edges and field, go through all cracks with a 4-inch V-blade wheel and scrape through joints before vacuuming.

- Make sure ALL dust has been vacuumed out of joints, corners, and cracks for next coating steps.

### Troubleshooting Common Issues

- Glazing: Caused by too much head pressure or wrong diamond bond. Drop down to a different bond diamond with the same size, or use water/sand to clean diamonds. They will not clean themselves.

- Gouging: Caused by sitting too long in one spot. Move faster or move up a diamond bond (less aggressive).

- Not cutting: Drop down a diamond bond and go back over everything to keep a continuous scratch pattern.

- Grinder stops running: Check propane cylinder for frozen linkage or empty tank. Replace tank and restart.

- Grinder is bogging: Check propane and follow same steps as above.

- Hand grinder turns off: Check generator and cords for disconnections or popped fuse.

- Vacuum has no suction: Purge vacuum, check and clean filter, shake hose for lodged dust, check and replace longo packs if too full.

## Revision History

| Date | Author | Changes |
| --- | --- | --- |
| 2026-04-13 | Dylan Nordby / SOP Manager | Initial version created from training documentation. |

Source: SOP Hub | Generated 2026-04-13