# Flake System Installation

| SOP ID | PEC-OPS-009 |
| --- | --- |
| Company | Prescott Epoxy Company (PEC) |
| Department | OPS |
| Version | 1.0 |
| Effective Date | 2026-04-13 |
| Owner | Dylan Nordby |

## Purpose

Standardize flake broadcast technique, coverage rates, and cleanup procedures to ensure full coverage and a clean final product.

## Scope

All PEC installers performing flake broadcast systems.

## Tools and Materials

- Simiron 1100 SL epoxy (base + medium cure activator)

- Flake material (0.125 lbs per sq ft)

- Flake buckets

- Leaf blower (if needed)

- Scraping tools

- Vacuum

- Polyaspartic topcoat materials

- Swing machine with red pad (for scrape day)

- PPE (gloves, respirators, glasses)

## Procedure

### Basecoat Application

Lay your Simiron 1100 SL product down at 160 square feet per gallon.

Refer to PEC-OPS-005 Simiron 1100 SL Product Training for full mixing and application instructions.

### Flake Broadcast Technique

- Flake is spread at a rate of around 0.125 lbs per square foot, which equates to around 320 square feet of floor space per box. Aim for full coverage to rejection when flaking.

- Throw high in the air with a flick in your wrist, allowing the flake to spread through the air and avoiding large clumps falling on the floor.

- Throwing less flake higher in the air at first helps cover more area rather than throwing a full bucket in one square.

- Try to overlap your throws and cover every spot where epoxy is shining through.

- Plan to have a little extra after the initial pass to go back over any light spots where flake may have sunk or was not covered.

- DO NOT walk back into flaked product as it can leave scratches and/or bare spots.

- As one person is flaking, another can be cleaning up the mixing station and filling buckets for consistent supply.

- One 40 lb box fills around 2.5 buckets of flake. Keep at least 2 buckets in rotation.

### Next Day Scrape and Cleanup

- After flake has cured into the epoxy, return the next day.

- Scrape one way and cross scrape to clean up any dead flake on top.

- Scrape into a pile.

- Clean up flakes that are bigger than 1/8 inch.

- Vacuum up everything that does not meet that size standard, as smaller contaminants create issues in future floors.

- If too many contaminants (leaves, pine needles, dust) get into the flake, check with the office. If given the go-ahead, throw it away.

### Topcoat Application

After flake cleanup, prepare your mixing station for polyaspartic coating.

Follow the steps in PEC-OPS-004 Polyaspartic HS Product Training for topcoat application using necessary tooling and PPE.

### Common Mistakes to Avoid

- Throwing too much flake in one area instead of spreading high and thin.

- Walking back into flaked product, causing scratches or bare spots.

- Not having enough buckets in rotation, causing delays.

- Not scraping and vacuuming thoroughly the next day, leaving contaminants under the topcoat.

- Using contaminated flake with leaves, pine needles, or excessive dust.

## Revision History

| Date | Author | Changes |
| --- | --- | --- |
| 2026-04-13 | Dylan Nordby / SOP Manager | Initial version created from training documentation. |

Source: SOP Hub | Generated 2026-04-13