# Metallic System Installation

| SOP ID | PEC-OPS-010 |
| --- | --- |
| Company | Prescott Epoxy Company (PEC) |
| Department | OPS |
| Version | 1.0 |
| Effective Date | 2026-04-13 |
| Owner | Dylan Nordby |

## Purpose

Provide step-by-step procedures for metallic system installation from prep through topcoat to ensure consistent, high-quality metallic floor finishes.

## Scope

All PEC installers performing metallic epoxy systems.

## Tools and Materials

- Simiron 1100 SL (clear base + slow cure activator)

- Metallic pigment (pre-mixed 24 hours prior)

- Base coat epoxy (color matched)

- Swing machine with red pad and 80 grit sanding screens

- 120 grit sanding screens

- Vacuum (nozzle that will not scratch)

- Acetone and rags

- High Wear Urethane topcoat

- Weenie roller

- 18-inch roller

- Tape

- 16/18 diamonds for grinding

- Epoxy paste patch materials

- PPE (gloves, long sleeves, glasses, respirators)

- Cleats

## Procedure

### Day Before: Metallic Pigment Prep

The day before the job, mix your metallic pigment into the clear epoxy using all necessary PPE (gloves, long sleeves, glasses, respirators).

Allow it to sit for as long as possible. The mica powder can create "shooting stars" if not thoroughly mixed.

### Surface Preparation

- Grind with 16/18 diamonds. Try for an extremely consistent grind throughout the floor.

- After grinding, patch every inconsistency: cracks, spalls, pin holes, or any contamination.

- Any contamination in the floor can cause outgassing and an inconsistent coating.

### Base Coat Application

Metallic systems go over a base coat epoxy that matches/compliments the metallic top coat.

Spread the base coat at 160 sq ft per gallon.

Allow to cure.

### Base Coat Sanding (Next Day)

- Bring a swing machine with a red pad and tan/red bristle brush with 80 grit sand paper screens.

- Sand until the sheen is completely gone and you are left with a matte finish on the base coat.

- After sanding, vacuum extremely well and do a thorough acetone wipe.

- Take note of any inconsistencies and patch with epoxy paste. Make sure patches are flush so no clear shows through the metallic.

- Allow patches to fire off enough to tack up without flowing/pulling when you go back over them.

### Metallic Coat Application

- Mix metallic pigmented epoxy with slow cure activator.

- Spread at a rate of 33-54 square feet per gallon (produces a yield of 30-48 mils per batch).

- Use a weenie roller around edges first. Do not roll, but push the product around to create the flowing effect of the mica powder.

- Use an 18-inch roller in the field. Push product in circles or random swirls, no further than 162 square feet per kit.

- Do not mess with the epoxy too much during application. Overworking can cause premature fire-off.

- Tape off the end of the floor so metallic does not flow past the desired area.

- Leave the epoxy to level and fire off for a smooth floor surface.

### Topcoat Preparation and Application

- After the metallic has thoroughly cured, bring the swing machine in with 120 grit sanding screen.

- Vacuum with a vacuum nozzle that will not leave scratches (scratches will be visible in the final product).

- Do a thorough acetone wipe.

- Proceed with High Wear Urethane topcoat using proper PPE (see PEC-OPS-003).

- Clean the jobsite thoroughly.

- Bring the customer in for a final look and give them the rundown on curing time.

### Common Mistakes to Avoid

- Not pre-mixing metallic pigment 24 hours ahead, causing shooting stars.

- Inconsistent grinding, leading to visible variation under the metallic.

- Not patching every pin hole and crack, causing outgassing.

- Using a vacuum nozzle that scratches the sanded metallic surface.

- Overworking the metallic during application, causing premature fire-off.

- Not taping off the end of the floor, allowing metallic to flow past the desired area.

## Revision History

| Date | Author | Changes |
| --- | --- | --- |
| 2026-04-13 | Dylan Nordby / SOP Manager | Initial version created from training documentation. |

Source: SOP Hub | Generated 2026-04-13